Dreamwalls® Backpainted Glass by Gardner Glass Products is an opportunity for architects and interior designers to add incredible color to interior environments. The advantages of Dreamwalls® Backpainted Glass include reflecting light and luminosity in a practical and easy-to-install material. It is easy to clean, hygienic, and durable due to Dreamwalls® unique application and heat-curing process. Dreamwalls® stands behind every piece with a 5-year warranty.

Dreamwalls® Backpainted Glass is manufactured using a two-coat proprietary paint technology developed specifically for superior adhesion to glass. The color coating is applied to the “second surface” or non-contact surface, of the glass, and heat-cured for exceptional durability. After installation, the color coating is not subject to degradation over time.

Extensive testing has been conducted on this coating to verify its reliability. It has shown superior resistance to color fading by UV light, non-yellowing properties, excellent resistance to a wide range of chemicals, cleaners, and moisture and humidity.

Colors are developed using a computerized intermix system with a database of over 25,000 colors. Virtually any non-metallic color can be produced with extremely accurate and repeatable results.

Dreamwalls® Backpainted Glass is manufactured using 6 mm (1/4-inch) Starphire® Ultra Clear by Vitro. This low-iron glass allows the color to be perfect without any greenish tint found in standard glass. This is particularly important for true reds, true whites, pastels, and creams to keep colors warm and true. Vitro Solargray® is used for glass with black coatings.

Gardner Glass Products are experienced fabricators of glass products with nationwide distribution. For further information, contact Dreamwalls® by Gardner Glass Products, Inc., North Wilkesboro, NC, (800) 334-7267, www.dreamwalls.com.

Specifier: This document is organized according to CSI MasterFormat and SectionFormat. Bold items require specifier selection. Convert bold to plain text, delete brackets, and removed specifier notes before publishing. Environmental requirements are shown in green and must be edited based on project requirements. This document is compatible with MASTERSPEC and SpecText editing tools.

Dreamwalls® is a registered trademark of Gardner Glass Products, Inc.

Starphire® and Solargray® are registered trademarks of Vitro Architectural Glass.

SECTION 088113

DECORATIVE GLASS GLAZING

GENERAL

Section Includes

Back painted glass for interior applications.

Related requirements

Specifier: Retain this optional Article and edit to provide cross reference to related work results in other sections. Section 088126 Interior Glass Glazing and Section 101116 Markerboards are available from Dreamwalls®.

Division 01 Section "Sustainable Design Requirements" for general sustainable design requirements including LEED requirements that apply to work of this Section.

Division 08 Section "Glazing" for standard glass products.

Division 08 Section "Mirrors" for mirror glass.

Section 088126 Interior Glass Glazing for laminated and tempered glass for interior applications.

Section 101116 Markerboards for glass whiteboards and color markerboards.

reference standards

References, General: Versions of the following standards current as of the date of issue of the project or as required by applicable code apply to the Work of this Section.

Specifier: Retain this optional article and edit to identify standards referenced elsewhere in the Section. Note that inclusion of a standard in this list does not require compliance with that standard; it must also be cited in the Section text.

ASTM International (ASTM):

ASTM C650 - Standard Test Method for Resistance of Ceramic Tile to Chemical Substances.

ASTM C1036 - Standard Specification for Flat Glass.

ASTM D870 - Standard Practice for Testing Water Resistance of Coatings Using Water Immersion.

ASTM D2197 - Standard Test Method for Adhesion of Organic Coatings by Scrape Adhesion.

ASTM D3359 - Standard Test Methods for Measuring Adhesion by Tape Test.

ASTM D3363 - Standard Test Method for Film Hardness by Pencil Test.

ASTM D4587 - Standard Practice for Fluorescent UV-Condensation Exposures of Paint and Related Coatings.

United States Green Building Council (USGBC):

LEED Green Building Rating System.

ADMINISTRATIVE REQUIREMENTS

Specifier: Retain one or both paragraphs below if complexity of back painted glass work justifies requirements.

Preinstallation Meetings: Conduct pre-installation conference at the site to coordinate Work of this Section with related work.

Sequencing: Schedule installation of back painted glass to follow adjacent work against which glass terminates. Schedule installation to follow nearby work whose execution may damage completed back painted glass work.

ACTION SUBMITTALS

Specifier: Action submittals require responsive action by Architect.

Product Data: Submit manufacturer's printed data sheets or catalog pages illustrating back painted glass products and accessories.

Specifier: Retain requirement below when Shop Drawings are required due to complexity of application; delete when Drawings adequately indicate layout of back painted glass work.

Shop Drawings: Submit shop drawings prepared specifically for the Project illustrating layout, edge details, dimensions, and other data necessary for satisfactory installation that are not shown in the contract documents.

Indicate back painted glass types with same designations used in this Section.

Samples: In manufacturer’s standard size.

Specifier: Retain first subparagraph below if back painted glass color selections are not indicated in Part 2.

Initial selection sample for each back painted glass type.

Verification samples for each back painted glass type.

Exposed fasteners.

INFORMATIONAL SUBMITTALS

Specifier: Informational submittals do not require responsive action by Architect.

Manufacturers' Instructions: Submit handling, storage, and installation instructions.

Sustainable Design Submittals: Submit certifications required in Quality Assurance Article.

Warranty: Sample of proposed manufacturer warranty.

CLOSEOUT SUBMITTALS

Maintenance data for back painted glass.

QUALITY ASSURANCE

Specifier: Retain paragraph below for projects intended to be LEED-certified and back painted glass is installed using adhesives. Add additional requirements that apply. Refer to USGBC LEED Reference Guide for detailed information.

Sustainability Standards Certifications: Provide the following LEED Submittals:

Credit EQ 4.1: Product data for adhesives, including printed statement of VOC content.

Specifier: Retain paragraph below when layout, patterns, or substrate present installation quality challenges best addressed by viewing of field mockups.

Mock-ups: Build mockup of each type of back painted glass installation to demonstrate quality standards for installation.

Approved mockups may be incorporated in the completed Work.

DELIVERY, STORAGE, AND HANDLING

Delivery and Acceptance Requirements: Deliver materials to project site in original sealed packages, with manufacturer's label, and with storage and handling directions.

Storage and Handling Requirements: Store and handle materials in accordance with manufacturer's instructions.

Store in clean, dry location with adequate ventilation for air circulation.

Protect from damage from weather, excessive temperature, and construction operations.

WARRANTY

Special Warranty: On manufacturer’s standard form in which manufacturer agrees to replace back painted glass products which lose functionality due to the deterioration or degradation of the color coated backing within specified warranty period.

Warranty Period: 5 years from date of Substantial Completion.

PRODUCTS

MANUFACTURERS

Manufacturer: Project design is based upon products fabricated by Gardner Glass Products, Inc., North Wilkesboro, NC, (800)334-7267, www.dreamwalls.com.

Substitution Limitations: Provide basis of design product or comparable product approved by Architect [prior to bid] [in accordance with Division 01 requirements].

Specifier: Copy this Article and re-edit as many times as required for each type of back painted glass. Create unique identifiers (e.g., BPG#1, BPG#2, etc.) for each type. Verify that Drawings identify and show location of each type. Contact Dreamwalls® for assistance in editing.

BACK PAINTED GLASS (BPg#_)

Back Painted Glass: Mirror-quality glass with heat-cured paint coating applied to second surface.

Basis of Design Product: Gardner Glass Products, Inc., Dreamwalls® Backpainted Glass.

Specifier: Virtually limitless range of colors are available. Color match from any specification (Pantone, Sherwin Williams, Benjamin Moore, RAL, etc.). Spectrophotometer color match available.

Color: <Insert color>.

Specifier: Maximum size is 100 x 144 inches.

Size: <Insert size>.

Specifier: Retain one finish below.

Classic Glossy is by far Dreamwalls’ bestseller, adding that sharp, shiny look to any interior space that only glass can give.

Matte adds a soft feel, reduces glare, minimizes fingerprints, and never washes off.

Prosuede© is a back painted, acid-etched glass that is fully dry erasable, and is 30% more scratch-resistant than regular glass.

Metallic and pearlescent finishes also available. See Dreamwalls® website for additional information or contact your Dreamwalls® sale representative.

Glass Finish: [Classic Glossy] [Matte (Acid Etched)] [Prosuede©].

Specifier: Dreamwalls® recommends using mechanical fasteners in addition to adhesive for mounting large back painted glass units. Select applicable Attachment Methods in subparagraphs below. Edit Accessory and Installation Articles to match.

Attachment Methods: [Adhesive] [Channels and adhesive] [Clips and adhesive] [Stand-offs].

Specifier: Verify graphics are shown on Drawings or delete if none.

Graphics: As indicated on Drawings.

Specifier: Verify cutouts and penetrations are shown on Drawing or delete if none.

Cutout and Penetrations: As indicated on Drawings.

Specifier: Standard edge for back painted glass is flat polished but seamed and other polishing options are available. Contact Dreamwalls® for additional information.

Glass Edge Treatment: Flat polished.

PERFORMANCE criteria

Provide back painted glass meeting or exceeding the following physical characteristics:

Coating Adhesion: ASTM D3359: 5 of 5.

Water Immersion, 65 deg. C, 40 days: ASTM D870: Pass.

Hardness: ASTM D3363: Pass 1H pencil after 24-hour aging.

Scratch Test: ASTM D2197: Pass 1.9 kg weight.

UV Resistance: ASTM D4587 313 Method, second surface: Pass 1000 hours.

Chemical Resistance: ASTM C650: Pass vinegar alkali test.

MATERIALS

Glass for White and Color Coatings: ASTM C1036, Mirror Select Quality; ultra-clear (low iron) float glass with a minimum 91 percent visible light transmission.

Basis of Design Product: PPG Industries, Inc., Starphire® Ultra-Clear Mirror.

Nominal Thickness: 6 mm (1/4 inch).

Glass for Black Coating: ASTM C1036, Mirror Glazing Quality.

Basis of Design Product: PPG Industries, Inc., Solargray®.

Nominal Thickness: 6 mm (1/4 inch).

Tint Color: Gray.

Specifier: With the only heat curing paint process in the industry, Dreamwalls® coatings provide exceptional protection against damage or deterioration.

Coating: Heat-cured acrylic epoxy and protective paint layers applied to second surface.

Specifier: Coordinate paragraphs below with mounting method indicated in Installation Article. If Adhesive Paragraph is retained, retain option for projects with interior VOC limits such as LEED projects or modify as required.

Adhesive: Adhesive setting compound, asbestos-free, certified by both back painted glass manufacturer and adhesive manufacturer as compatible with glass coating and substrates. [Use adhesive with VOC content of 70 g/L or less per 40 CFR 59, Subpart D (EPA Method 24).]

Channels: Manufacturer’s standard [clear anodized aluminum] [bronze anodized aluminum] [chrome-plated steel] [nickel-plated steel] [stainless steel] [brass] <insert other color anodized or powder coated finish>, matched set of bottom and top channels, size to match glass thickness.

Stand-Offs: Manufacturer’s standard [chrome-plated steel] [nickel-plated steel] [stainless steel] [brass] standoffs.

Z-Clips: Manufacturer’s standard.

EXECUTION

EXAMINATION

Verification of Conditions: Verify that substrates to receive back painted glass are plumb, level, smooth, clean, dry, and sound. Correct deficiencies prior to commencing installation.

Verify compatibility of proposed adhesives with substrate.

PREPARATION

Surface Preparation: Comply with adhesive manufacturer's recommendations. Correct minor defects in substrate using leveling compounds acceptable to both back painted glass manufacturer and adhesive manufacturer. Prime substrate where recommended.

INSTALLATION

Specifier: Retain option in paragraph below if Shop Drawings are required in Action Submittals Article.

General: Install back painted units in accordance with manufacturer's recommendations[ and approved shop drawings].

Specifier: Retain one of four Installation paragraphs below.

Adhesive Installation: Apply barrier coat to back painted glass when recommended by adhesive manufacturer. Apply adhesive as recommended by manufacturer. Align back painted glass units and press into place.

Specifier: For large back painted glass units, Dreamwalls recommends using mechanical fasteners in addition to adhesive.

Channels and Adhesive Installation: Install set of channels along bottom and top of installation, adjusting so channels are level and evenly spaced. Cut back painted glass to exact length required to set into channels with full support. Apply adhesive to substrate and set glass as recommended by manufacturer.

Z-Clips and Adhesive Installation: Install using z-clips, adjusting so back painted glass is level. Apply adhesive to substrate and set glass as recommended by manufacturer.

Stand-Off Installation: Drill hole in glass sized to accommodate sleeve, felt washer, stand-off, and screw at each corner of glass units, located minimum 3 inches (75 mm) from edge of glass. Do not allow screw to touch glass. Do not use adhesive. Hand-tighten screws.

Tolerances: Install back painted glass to allow for anticipated structural movement. Space selected units 1/32 inch (1 mm) horizontally, with blackened substrate where vertical joint may open over time. Allow for vertical settling between back painted glass units and adjacent components.

cleaning

Wash exposed surfaces of back painted glass as recommended by manufacturer not more than three days prior to scheduled inspection for Substantial Completion.

PROTECTION

Protect back painted glass from damage resulting from construction activities.

Remove and replace broken or damaged glass.

END OF SECTION

Additional Specifiers Notes

Substitution Reviews: When reviewing substitution requests for other products for compliance with this specification, Dreamwalls® recommends particular attention to the following issues:

Quality of glass substrate.

Range of available colors.

Performance characteristics of applied coating.

Terms and conditions of available warranty.

Coordination with Drawings: Make sure you coordinate the following:

Location of each back painted glass unit, using designations from specification or schedule.

Size and shape of each unit, and sizes, shapes, and locations of cutouts and notches.

Detail of edges.

Method of mounting or support.